**Product Description**

Premium quality electrical self-extinguishing soft PVC tape with a rubber adhesive

**Applications**

Predominantly electrical insulation, also colour coding and for electrical cables wrapping in automotive application.

**Features & Benefits**

Good resistance to abrasion, corrosion and moisture

High dielectric strength

Excellent conformability

Conforms to BS3924 replaced by EN 60454-3-12:2006

Conforms to EN 60454-3-12:2006

IEC 62321:2008

2006/95/EC (Low Voltage Directive)

UL510 certificated (Flame Retardant)

**Technical Performance**

|  |  |  |  |
| --- | --- | --- | --- |
| Description | Units | Value | Test Method |
| Total thickness | mm | 0.13±0.005 | GB7125-1999 |
| Adhesive | - | Rubber | No residue |
| Elongation at break | % | ≥180 | GB7753-1987 |
| Tensile strength | N/cm | ≥22 | GB7753-1987 |
| Voltage breakdown | KV | 6 | EN 60454-4-3-12:2006 |
| Flammability | - | PASSED | UL510 |

**Declaration of Conformity Information**

EN 60454-3-12:2006, IEC 62321:2008, 2006/95/EC (Low Voltage Directive) BS3924, UL510

**REACH SVHC Status**

NO SHVC present according to candidates list of 15th June 2015

**RoHS Compliance Status**

2011/65/EU

**Storage Details**

Shelf life recommended 2 years from date of despatch at the moderate temperature and humidity environment.